**Sample Coverage Chart for Loose-Fill Insulation**

Blown Cellulose “Cocoontm” (25-lb. bag)

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Thickness** | **R-Value** | **Density/ft3** | **Weight/ft2** | **Bags/1,000ft2** | **Coverage** |
| 2 x 4 | 13 | 2.6 lbs | 0.75 lbs | 28 | 36 ft2 |
| 2 x 6 | 20 | 2.6 lbs | 1.192 lbs | 43 | 23 ft2 |

Blown Fiberglass CertainTeed “Optima” (27-lb. bag)

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Thickness** | **R-Value** | **Density/ft3** | **Weight/ft2** | **Bags/1,000ft2** | **Coverage** |
| 2 x 4 | 14 | 1.6 lbs | 0.46 lbs | 16.7 | 60 ft2 |
| 2 x 6 | 22 | 1.6 lbs | 0.73 lbs | 26.0 | 38 ft2 |